#### PART 1 – GENERAL

#### 1.01 Section Includes

- Sprayed cellulose thermal barrier insulation.

1.02	Related Items

- Clips, hangers, supports, sleeves and other attachments to spray bases are to be placed by other trades prior to the application of sprayed insulation.

- Ducts, piping, conduit or other suspended equipment shall not be positioned until after the application of sprayed insulation.

- Roof penetrations to be installed prior to application.

1.03   Quality Assurance

- Manufacturer must have a current Underwriters Laboratories (UL) Code Evaluation Report.

- Manufacturer must be in compliance with the 2009 and 2012 International Building Code.

- Manufacturer must be ISO 9001:2015 Certified.

- Applicator:  Licensed by manufacturer.

- Manufacturer must subscribe to independent laboratory follow-up inspection services of   Underwriters Laboratories and Factory Mutual.  Each bag shall be labeled accordingly.

- Mock-up:  Apply a 100 square foot representative sample to be reviewed by the Architect   and/or Owner prior to proceeding.

1.04   Submittals

- Submit product data that the product meets or exceeds the following specified requirements.

- R-Value shall be 3.6 per inch per ASTM C 518.

- Bond strength shall be greater than 100 psf per ASTM E 736.

- Product shall be Class 1 Class A per ASTM E 84/ UL 723.

- Tested in accordance with UBC 26-2 Test Method for the evaluation of Thermal Barriers (ASTM E 119)

- NRC to be 0.95 @ 1.25” thick per ASTM E 1042.

- Pass Full – Scale Corner Test.

- Comply with 2009 IBC Section 803.10 stability requirements for interior finishes.

- Manufacturer's written certification that product contains no asbestos, fiberglass or other man-made mineral fibers.

- Copy of manufacturer’s ISO 9001:2015 Certification.

- Minimum Fiber Recycled Content to be 75%.

- Cannot contain any added Urea-Formaldehyde Resins.

1.05	Delivery, Storage and Handling

- Deliver in original, unopened containers bearing name of manufacturer, product identification and reference to U.L. testing.

- Store materials dry, off ground, and under cover.

- Protect liquid adhesive from freezing.

# PART 2 – PRODUCTS

2.01	Acceptable Manufacturers

- International Cellulose Corporation

12315 Robin Boulevard

Houston, Texas 77045

(713) 433-6701 or (800) 444-1252

FAX:  (713) 433-2029

www.spray-on.com	icc@spray-on.com

- For approved applicators contact ICC at 800-444-1252.

2.02   Materials

- Ure-K Thermal Barrier System.

- Color shall be from Manufacturer’s standard color chart.

- Comply with local Building Code requirements.

##### PART 3 – EXECUTION

3.01   Examination

- Examine surfaces and report unsatisfactory conditions in writing.  Do not proceed until unsatisfactory conditions are corrected.

- Verify surfaces to receive spray insulation to determine if priming/sealing is required to insure bonding and/or to prevent discoloration caused by migratory stains.

  - Preparation

- Provide masking, drop cloths or other satisfactory coverings for materials/surfaces that are not to receive insulation to protect from over-spray.

- Coordinate installation of the sprayed cellulose fiber with work of other trades.

- Prime surfaces as required by manufacturer’s instructions or as determined by examination.

  - Installation

- Thickness will be determined as the minimum thickness measured as per ASTM E-605 field test procedure.

- Install spray applied insulation according to manufacturer’s recommendations.

- Install Thermal Barrier System at 1.25” average thickness.

- Cure insulation with continuous natural or mechanical ventilation.

- Remove and dispose of over-spray.

  - Protection

Protect finished installation under provision of Division 1.

# END OF SECTION